BAIYUN SS818 Silicone

Stain-Resistant Weather Proofing Sealant

FEATURES

- Non-staining on natural stones and reduces residue rundown on metal and glass panels

- Extension/compression movement capability of up to ±50% of the original joint width

- No unpleasant odor during curing

- Non-corrosive curing system

- Excellent weather-ability and high resistance to ultraviolet radiation, heat and humidity, ozone and temperature extremes

- Remains flexible over a temperature range of -58℉ (-50℃) to 302℉ (150℃)

- Excellent un-primed adhesion to wide range of substrates including coated, enameled and reflective glasses, anodized and polyester coated or painted aluminum profiles

- 10-year Limited Weather seal and Non-Staining Warranties are available

COMPOSITION

- One-part, neutral-curing

- RTV silicone sealant

APPLICATIONS

- Joint weather sealing of glass curtain wall

- Weather sealing in metal, enamel curtain wall joints

- No-staining for porous materials, e.g. concrete, cement, stone, etc.

- Minimize residence rundown streaking

TYPICAL PROPERTIES

| Property | Result | Test method |
| --- | --- | --- |
| As Supplied |  |  |
| Tack free time(23°C/73°F, 50% RH) | 55 minutes | ASTM C679 |
| Full Adhesion | 14-21 days |  |
| Flow, Sag or Slump | ＜0.1 mm | ASTM C639 |
| Working Time | 10-15 minutes |  |
| Specific Gravity | 1.34 | ASTM D1475 |
| VOC Content | ＜40 g/L |  |
| As Cured-After 7 days at 23°C (73°F) and 50% RH |  |  |
| Ultimate Tensile Strength | 1.7 MPa | ASTM D412 |
| Ultimate Elongation | 990% | ASTM D412 |
| As Cured-After 21 days at 23°C (73°F) and 50% RH |  |  |
| Durometer Hardness, Shore A | 25-40 | ASTM C661 |
| Joint Movement Capability | ±50% | ASTM C719 |
| Ultimate Tensile Strength | 0.8 MPa | ASTM C1135 |
| Ultimate Elongation | 450% | ASTM C 1135 |
| Staining and migration, natural stone | None | ASTM C1248 |
| Specifications: Typical property data values should not be used as specifications. Assistance with specifications are available by contacting Guangzhou Baiyun Technology CO.,LTD. |  |  |

SPECIFICATIONS

·ASTM C920; Type S, Grade NS, Class 50, Use NT, A, G, O

·ASTM C1248

·ISO 11600 class 25

·GB/T 23261 class 50

COLORS

Black, gray and white (general colors)

Other wide variety of colors (customized)

PACKAGING

300 mL cartridge and 590 mL sausage

USABLE LIFE AND STORAGE

12 months from the date of manufacture when stored at or below 27ºC (80ºF) in the original unopened containers.

LIMITATIONS

This product should not be used, applied or recommended:

- In structural glazing applications or where the sealant is intended as an adhesive

- In areas where abrasion and physical abuse are encountered

- In totally confined spaces as the sealant requires atmospheric moisture for cure

- On frost-laden or damp surfaces

- To building materials that bleed oils, plasticizers or solvents – materials such as impregnated wood, oil-based caulks, green or partially vulcanized rubber gaskets or tapes

- In below-grade applications

- On substrates made of polypropylene, polyethylene, polycarbonate and polytetrafluoroethylene

- Where movement capability greater than ±50% is required

- Where painting of the sealant is required, as the paint film may crack and peel

- For structural adhesion on bare metals or surfaces subject to corrosion (i.e., mill aluminum, bare steel, etc.)

- To surfaces in contact with food

- For use underwater or in other applications where the product will be in continuous contact with water

HANDLING AND SAFETY

PRODUCT SAFETY INFORMATION REQUIRED FOR SAFE USE IS NOT INCLUDED IN THIS DOCUMENT. BEFORE HANDLING, READ PRODUCT AND MATERIAL SAFETY DATA SHEETS AND CONTAINER LABELS FOR SAFE USE, PHYSICAL AND HEALTH HAZARD INFORMATION. THE MATERIAL SAFETY DATA SHEET IS AVAILABLE FROM BAIYUN SALES APPLICATION ENGINEER, OR DISTRIBUTOR, OR BY CALLING BAIYUN CUSTOMER SERVICE.

HOW TO USE

Complete design and installation guidelines are contained in the BAIYUN Technical Manual when using this product.

HEALTH AND ENVIRONMENT INFORMATION

For information and advice regarding transportation, handling, storage and disposal of chemical products, users should refer to the actual Material Safety Data Sheets containing physical, ecological toxicological and other safety-related data.