BAI YUN® SS628 Silicone Structural Sealant

Features

- High level of mechanic properties: High strength

- Non-corrosive curing system

- No unpleasant odor during curing

- Excellent weather ability and high resistance to ultraviolet radiation, heat and humidity, ozone and temperature extremes

- Remains flexible over a temperature range of -58 ºF (-50℃) to 302 ºF (150℃)

- Successfully tested for using in protective glazing applications

- Excellent unprimed adhesion to wide range of substrates including coated, enameled and reflective glasses, anodized and polyester coated or painted aluminum profiles

- Good compatibility with other neutral silicone sealants

Composition

- Two-part, neutral-curing

- RTV silicone sealant

Applications

- As a secondary edge adhesive sealant in insulating glass units

- Structural attachment of many panel systems

- Protective glazing applications

- Panel stiffener applications

Typical properties

| Property | Result | Test method |
| --- | --- | --- |
| Base-As Supplied |  |  |
| Color | White |  |
| Physical Form | Paste |  |
| Specific Gravity | 1.38 g/cm³ | ASTM D1475 |
| Catalyst-As Supplied |  |  |
| Color | Black |  |
| Physical Form | Viscous Paste |  |
| Specific Gravity | 1.04 g/cm³ | ASTM D1475 |
| As catalyzed |  |  |
| Color | Black |  |
| Specific Gravity | 1.35 g/cm³ | ASTM D1475 |
| Tooling Time(23°C/73°F, 50% RH) | 10-20 minutes |  |
| Snap time(23°C/73°F, 50% RH) | 20-70 minutes |  |
| Flow, Sag or Slump | ＜0.1mm | ASTM C639 |
| Mix Ratio(By volume) | A:B = 9-11:1 |  |
| Recommend Mix Ratio(By volume) | A:B=10:1 |  |
| VOC Content | ＜40 g/L |  |
| As cured - After 21 days at 23°C (73°F) and 50% RH |  |  |
| Durometer Hardness, Shore A | 40 | ASTM C661 |
| Ultimate Tensile Strength | 1.1MPa | ASTM C1135 |
| Ultimate Elongation | 170% | ASTM C1135 |
| Tear Strength ,Die B | 8 kN/m | ASTM D624 |
| Specifications: Typical property data values should not be used as specifications. Assistance with specifications are available by contacting Guangzhou Baiyun Technology CO., LTD. |  |  |

Specifications

·ASTM C1184, Type M, Use G and O

·GB 16776

Colors

Part A (Base): White,  Part B(Catalyst): Black,  After Mixed: Black

Package

Part A (Base): 189L/Drum

Part B (Catalyst): 19L/Drum

Storage and shelf life:

For Part A（Base）：18 months from the date of manufacture when stored at or below 27ºC (80ºF) in the original unopened containers.

For Part B（Catalyst）：12 months from the date of manufacture when stored at or below 27ºC (80ºF) in the original unopened containers.

Product limitation:

This product should not be applied:

- In structural glazing applications, unless Guangzhou Baiyun Technology CO., LTD. has reviewed shop drawings for applicability and has performed adhesion and compatibility tests on project substrates, spacer materials and all accompanying accessories. Review and testing is done on a project-by-project basis. No blanket approval is given by Guangzhou Baiyun Technology CO.,LTD. for structural glazing applications. Structural glazing industry guidelines (ASTM C1401) suggest that drawings and details are to be reviewed by all parties involved in the manufacture of an SSG system and for each building project.

- To building materials that bleed oils, plasticizers or solvents – materials such as impregnated wood, oil-based caulks, green or partially vulcanized rubber gaskets or tapes

- When surface temperatures below 10ºC (50ºF) or exceed 40ºC (104ºF)

- Where painting of the sealant is required, as the paint film may crack and peel

- In below-grade applications

- For use as an interior penetration fire stop sealing system

- In horizontal floor joints where abrasion and physical abuse are likely to be encountered

- To frost-laden or damp surfaces

- For structural adhesion on bare metals or surfaces subject to corrosion (i.e., mill aluminum, bare steel, etc.)

- For contact with strong acids or bases

- To surfaces in contact with food

- For continuous immersion in water

- For water immersion applications

Do not apply acid-curing (Acetoxy) silicone sealants to this product as this may cause loss of adhesion of SS628 Silicone Structural Sealant to glass or other substrates used in the system.

Handling and safety

Product safety information required for safe use is not included in this document. Before handling, read product and material safety data sheets and container labels for safe use, physical and health hazard information. The material safety data sheet is available from BAIYUN sales application engineer, or distributor, or by calling BAIYUN customer service.

How to use

BAIYUN SS628 Silicone Structural Sealant, when used in structural applications, must be reviewed by BAIYUN technical service specialists.

Complete design and installation guidelines are contained in the BAIYUN Technical Manual when using this product.

Health and environment information

For information and advice regarding transportation, handling, storage and disposal of chemical products, users should refer to the actual Material Safety Data Sheets containing physical, ecological toxicological and other safety-related data.